## Slide 1
Experiments with spin qubits in diamond

## Slide 2
Diamond
  Nitrogen-vacancy (NV-) centre
    1. Properties
    2. Applications
    a) magnetometry
    b) thermometry
    c) electrometry
    d) in a tractor beam?
    e) violating Bell’s inequality
  Silicon-vacancy (SiV) centre
Experiments with spin qubits in diamond: overview

## Slide 3
Diamond
EPSRC CDT:
Warwick (host)
Oxford
Imperial
Bristol
Cardiff
Strathclyde
Newcastle Aberystwyth
Diamond crystal structure. Page 37, Singleton, Band Theory and Electronic Properties of Solids, OUP 2001
Face-centred cubic (FCC)
with two atom basis

## Slide 4
Diamond
Schematic of the formation of sp3 hybrid bonding states in diamond. Page 37, Singleton, Band Theory and Electronic Properties of Solids, OUP 2001
- tight-binding model
Carbon:
1s2 2s2 2p2

## Slide 5
Diamond
Schematic of the formation of sp3 hybrid bonding states in diamond. Page 37, Singleton, Band Theory and Electronic Properties of Solids, OUP 2001
- tight-binding model
Carbon:
1s2 2s2 2p2
5.5 eV band gap
Diamond is an insulator:
”a place where electrons can be hermits”

## Slide 6
Diamond defects
F Bridges, G Davies, J Robertson and AM Stoneham, Journal of Physics-Condensed Matter 2, 2875 (1990)

## Slide 7
Diamond defects
F Bridges, G Davies, J Robertson and AM Stoneham, Journal of Physics-Condensed Matter 2, 2875 (1990)

## Slide 8
Diamond defects
F Bridges, G Davies, J Robertson and AM Stoneham, Journal of Physics-Condensed Matter 2, 2875 (1990)

## Slide 9
Diamond defects
F Bridges, G Davies, J Robertson and AM Stoneham, Journal of Physics-Condensed Matter 2, 2875 (1990)

## Slide 10
The nitrogen-vacancy (NV) centre in diamond
Confocal microscope image
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)

## Slide 11
Single nitrogen-vacancy centres
Hanbury Brown and Twiss (HBT) experiment
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
Correlation?
Detector 2
Detector 1
Green excitation

## Slide 12
Single nitrogen-vacancy centres
NV- optical spectroscopy
A Gruber, A Drabenstedt, C Tietz, L Fleury, J Wrachtrup*, C. von Borczyskowski, Science 276, 2012 (1997).
Green excitation in, red florescence out
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013).
See also: M Fox, Optical Properties of Solids, Second Edition, OUP 2013, Section 8.2, page 218-224.

## Slide 13
Single nitrogen-vacancy centres
NV- electron spin resonance spectroscopy
Optically-detected magnetic resonance (ODMR)
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)

## Slide 14
Single nitrogen-vacancy centres
NV- energy levels
JHN Loubser
& JA van Wyk, Rep Progr Phys 41 1202 (1978)
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)

## Slide 15
Single nitrogen-vacancy centres
NV- energy levels
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
3A2
3E
1A1
1E
±1
±1
±0
±0
Red names come from the C3v point group: see appendix of Doherty et al
Black numbers are spin state (in zero magnetic field)

## Slide 16
Single nitrogen-vacancy centres
NV- energy levels
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
3A2
3E
1A1
1E
±1
±1
±0
±0
Green excitation

## Slide 17
Single nitrogen-vacancy centres
NV- energy levels
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
3A2
3E
1A1
1E
±1
±1
±0
±0
Red Emission
Decay time ~10ns

## Slide 18
Single nitrogen-vacancy centres
NV- energy levels
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
3A2
3E
1A1
1E
±1
±1
±0
±0
Microwave excitation (2.9 GHz)

## Slide 19
Single nitrogen-vacancy centres
NV- energy levels
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
3A2
3E
1A1
1E
±1
±1
±0
±0
Green excitation

## Slide 20
Single nitrogen-vacancy centres
NV- energy levels
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
3A2
3E
1A1
1E
±1
±1
±0
±0
No florescence, ~300 ns decay time

## Slide 21
Single nitrogen-vacancy centres
NV- energy levels
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
Green excitation light polarizes the NV- electron spin far beyond Boltzmann polarization
Florescence intensity depends on spin state

## Slide 22
Single nitrogen-vacancy centres
NV- optically-detected magnetic resonance
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
Green excitation light polarizes the NV- electron spin far beyond Boltzmann polarization
Florescence intensity depends on spin state

## Slide 23
Single nitrogen-vacancy centres
NV- summary
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
Mini-overview
NV fabrication
Qubit initialisation
Readout
Control
Coherence times

## Slide 24
Single nitrogen-vacancy centres
Initialize nuclear spins as well as electrons
Mini-overview
NV fabrication
Qubit initialisation
Readout
Control
Coherence times
V Jacques et al, Physical Review Letters 102, 057403 (2009)

## Slide 25
Single nitrogen-vacancy centres
Single shot readout using nuclear spins
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
Mini-overview
NV fabrication
Qubit initialisation
Readout
Control
Coherence times
L. Jiang et al, Science 326, 267 (2009)
P Neumann et al, Science 329, 542 (2010)
E Togan et al, Nature 478, 497 (2011)

## Slide 26
Single nitrogen-vacancy centres
Quantum control of electron and nuclear spins
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
Mini-overview
NV fabrication
Qubit initialisation
Readout
Control
Coherence times
Microwaves to control electron spin and
radiowaves to control nuclear spins
eg three spin quantum error correction:
G Waldherr et al, Nature 506, 204 (2014)

## Slide 27
Single nitrogen-vacancy centres
Ion implantation for fabrication
Mini-overview
NV fabrication
Qubit initialisation
Readout
Control
Coherence times
Very imperfect arrays:
up to 50% yield for NV- after nitrogen ion implantation
Worse for shallow NV-
~50 nm precision
Repeat-until-success?
DM Toyli et al, Nano Lett 10, 3168 (2010)

## Slide 28
Single nitrogen-vacancy centres
Laser-writing for fabrication
Very imperfect arrays:
up to 50% yield for NV-
Worse for shallow NV-
~200 nm precision
Repeat-until-success?
Courvoisier, Booth, and Salter, APL 109, 031109 (2016)
Chen, Salter, Knauer, Weng, Frangeskou, Stephen, Ishmael, Dolan, Johnson, Green, Morley, Newton, Rarity, Booth, Smith, Nat Photon 11, 77 (2017)

## Slide 29
Single nitrogen-vacancy centres
Spin coherence times
Mini-overview
NV fabrication
Qubit initialisation
Readout
Control
Coherence times
 | Electron spin in 12C | Nuclear spin
Room temperature T2 | 1.8 ms | 1 s
Cryogenic T2 | 0.6 s (77 K with dynamic decoupling) | 10 s (at 8 K)
1.8 ms: G Balasubramanian et al, Nature Materials 8, 383 (2009)
0.6 s: N Bar-Gill et al, Nat Commun 4, 1743 (2013)
1 s: PC Maurer et al, Science 336, 1283 (2012)
10s: S Yang et al, Nat Photon 10, 507 (2016)

## Slide 30
Single nitrogen-vacancy centres
Properties
Mini-overview
NV fabrication
Qubit initialisation
Readout
Control
Coherence times
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)

## Slide 31
Nitrogen-vacancy centres: Applications
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
Magnetometer, Electrometer, Thermometer…

## Slide 32
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 33
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 34
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 35
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 36
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 37
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 38
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 39
Classical Sensing
With classical sensors, the signal to noise improves as
(for random noise i.e. the signal is uncorrelated to the noise, and the noise is uncorrelated)
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 40: Sensitivity
The minimal change in the measured quantity that can be resolved above the noise
A quantity (e.g. a magnetic field in Tesla) is measured as B, and its uncertainty in a single measurement is δB. Averaging over N measurements gives the average:
,
and its uncertainty:

## Slide 41: Sensitivity (cont.)
(1) The signal to noise ratio,
(2) The number of measurements is the measurement rate (R ) times the total measurement time (T ): N = R T , so
.
We define the sensitivity in measuring B as:
,
which has units of [B ].Hz-½ so for a magnetic field sensor it’s T.Hz-½

## Slide 42
Quantum Sensing
UΦ
UΦ
Use superposition
Use entanglement
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 43
Quantum Sensing
classical sensors: SNR improves as
quantum sensors: SNR can improve as
But it requires entanglement, and imperfections lower the quantum advantage
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 44
Practical Quantum Sensing
Don’t use maximally entangled states because of decoherence
Quantum sensing is useful when averaging is limited e.g. by size, time, fragile samples
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 45
Practical Quantum Sensing
  Magnetometry
  Thermometry
  Accelerometers
  Gravimetry
  Microscopy
  Imaging
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 46
Nitrogen-vacancy centres: Applications
MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)
Magnetometer, Electrometer, Thermometer…

## Slide 47
Nitrogen-vacancy centres: Applications
DC Magnetometer
Energy of NV- with spin 1
Magnetic field, B0
ms = +1
ms = -1
ms = 0
2.88 GHz
Review:
L Rondin et al., Magnetometry with nitrogen-vacancy defects in diamond, Rep Prog Phys 77, 056503 (2014)

## Slide 48
Nitrogen-vacancy centres: Applications
DC Magnetometer
Energy of NV- with spin 1
Magnetic field, B0
ms = +1
ms = -1
ms = 0
- lock-in detection
- large ensemble of NV- (sacrificing nanoscale spatial resolution)
- multiple passes of light though the diamond
15 pT.Hz-½ sensitivity at 80 - 2000 Hz from (13 x 200 x 2000) µm3 diamond: JF Barry et al., PNAS 2016

## Slide 49
Lock-in detection
Magnetic field, B
Magnetic field modulation
(~1 to 100 kHz)
Advantage: noise only at
modulation frequency
Signal
Lock-in signal
Bulk, DC, lock-in

## Slide 50
Nitrogen-vacancy centres: Applications
DC Magnetometer: lock-in detection
H Clevenson et al, Nat Phys 11, 393 (2015)
Bulk, DC, lock-in

## Slide 51
15 pT.Hz-½ sensitivity at 80 - 2000 Hz from (13 x 200 x 2000) µm3 diamond: JF Barry et al., PNAS 2016
Nitrogen-vacancy centres: Applications
DC Magnetometer
Bulk, DC, lock-in

## Slide 52
Nitrogen-vacancy centres: Applications
DC Magnetometer
- lock-in detection
- ensemble of ~1013 NV- (sacrificing nanoscale spatial resolution)
300 pT/√Hz sensitivity at 1 Hz:
H Clevenson et al, Nat Phys 11, 393 (2015)
15 pT/√Hz sensitivity at 80 - 2000 Hz:
JF Barry et al, PNAS 113, 14133 (2016)
Comercial viability:
MW Dale & GWM, arXiv:1705.01994 (2017)
Barry et al

## Slide 53
Single nitrogen-vacancy centres
Ramsey interferometry
Review:
L Rondin et al., Magnetometry with nitrogen-vacancy defects in diamond, Rep Prog Phys 77, 056503 (2014)
Bulk, DC, beyond lock-in

## Slide 54
Review:
L Rondin et al., Magnetometry with nitrogen-vacancy defects in diamond, Rep Prog Phys 77, 056503 (2014)
Single nitrogen-vacancy centres
AC magnetometry
AC, pulsed readout

## Slide 55
Spin echo
In rotating frame
Spin echo
AC, pulsed readout
Notes: Hahn echo

## Slide 56
Spin echo
In rotating frame
Spin echo
AC, pulsed readout
Notes: Hahn echo

## Slide 57
Nitrogen-vacancy centres: Applications
AC Magnetometer
- Spin echo on the NV- centre allows through chosen frequency of interest
- Control noise in laser and microwave sources
- Ensemble of ~1011 NV-
0.9 pT/√Hz sensitivity at 10 kHz:
T Wolf et al, PRX 5, 041001 (2015)

## Slide 58
Single nitrogen-vacancy centres
Spin coherence times
 | Electron spin in 12C | Nuclear spin
Room temperature T2 | 1.8 ms | 1 s
cryogenic T2 | 0.6 s (77 K with decoupling) | 10 s (at 8 K)
1.8 ms: G Balasubramanian et al, Nature Materials 8, 383 (2009)
0.6 s: N Bar-Gill et al, Nat Commun 4, 1743 (2013)
1 s: PC Maurer et al, Science 336, 1283 (2012)
10 s: S Yang et al, Nature Photonics 10, 507 (2016)
AC, pulsed readout

## Slide 59
Warwick: single spin magnetometry
Nitrogen-vacancy centres: Applications
Single NV, AC, pulsed readout

## Slide 60
Nitrogen-vacancy centres: Applications
Nanoscale AC magnetometer for single spin NMR
- Spin echo on the NV- centre allows through chosen frequency of interest
- Single NV- detects a reporter spin
Single proton spin on surface of diamond:
AO Sushkov et al, Phys Rev Lett 113, 197601 (2014)

## Slide 61
Nanoscale magnetometer for scanning over a sample
Nitrogen-vacancy centres: Applications
P. Maletinsky et al., Nature Nano. 7, 320 (2012)
Single NV, AC, pulsed readout

## Slide 62
Nitrogen-vacancy centres: Applications
Nanoscale AC magnetometer for scanning over a sample
- Dynamic decoupling allows through chosen frequency of interest
- The electron spin being detected was another NV-
Detect a single electron spin 50 nm away from NV- sensor:
MS Grinolds et al, Nat Phys 9, 215 (2013)

## Slide 63
Nitrogen-vacancy centres: Applications
Wide-field magnetometry
Optical magnetic imaging of living cells, D Le Sage et al, Nature 496, 486 (2013)
Diamond is bio-compatible

## Slide 64
Nitrogen-vacancy centres: Applications
High resolution: Qdyne
S Schmitt et al, Science 356, 832 (2017)
JM Boss et al, Science 356, 837 (2017)

## Slide 65
Nitrogen-vacancy centres: Applications
High resolution: Qdyne
DB Bucher et al, arXiv:1705.08887 (2017)

## Slide 66
Nitrogen-vacancy centres: Applications
Nanoscale thermometry for inside living cells & computer chips
G Kucsko et al, Nature 500, 54 (2013)
P Neumann et al, Nano Lett 13, 2738 (2013)
DM Toyli et al, PNAS 110, 8417 (2013)
with
and βT = 74 kHz/K

## Slide 67
Nitrogen-vacancy centres: Applications
Electrometry: Stark shift
F Dolde et al, Nat Phys 7, 459 (2011)

## Slide 68
Nitrogen-vacancy centres: Applications
In a tractor beam
Proposals:
- M Scala et al, PRL 111, 180403 (2013)
- Z-q Yin et al, PRA 88, 033614 (2013)
- C Wan et al, PRL 117, 143003 (2016)
Experiments:
- LP Neukirch et al, Nat Photon 9, 653 (2015)
- AC Frangeskou et al., arXiv:1608.04724 (2016)

## Slide 72
From our collaboration:
- M Scala et al., PRL 111, 180403 (2013)
- C Wan et al., PRA 93, 043852 (2016)
- C Wan et al., PRL 117, 143003 (2016)
From other groups:
- Z-q Yin, T Li, X Zhang & LM Duan,
PRA 88, 033614 (2013)
  Our proposal:
  drop a nanodiamond containing a spin

## Slide 73
From our collaboration:
- M Scala et al., PRL 111, 180403 (2013)
- C Wan et al., PRA 93, 043852 (2016)
- C Wan et al., PRL 117, 143003 (2016)
  Our proposal:
  drop a nanodiamond containing a spin

## Slide 74
From our collaboration:
- M Scala et al., PRL 111, 180403 (2013)
- C Wan et al., PRA 93, 043852 (2016)
- C Wan et al., PRL 117, 143003 (2016)
  Our proposal:
  drop a nanodiamond containing a spin

## Slide 75
From our collaboration:
- M Scala et al., PRL 111, 180403 (2013)
- C Wan et al., PRA 93, 043852 (2016)
- C Wan et al., PRL 117, 143003 (2016)
  Our proposal:
  drop a nanodiamond containing a spin

## Slide 76
From our collaboration:
- M Scala et al., PRL 111, 180403 (2013)
- C Wan et al., PRA 93, 043852 (2016)
- C Wan et al., PRL 117, 143003 (2016)
  Our proposal:
  drop a nanodiamond containing a spin

## Slide 77
From our collaboration:
- M Scala et al., PRL 111, 180403 (2013)
- C Wan et al., PRA 93, 043852 (2016)
- C Wan et al., PRL 117, 143003 (2016)
  Our proposal:
  drop a nanodiamond containing a spin

## Slide 78
From our collaboration:
- M Scala et al., PRL 111, 180403 (2013)
- C Wan et al., PRA 93, 043852 (2016)
- C Wan et al., PRL 117, 143003 (2016)
  Our proposal:
  drop a nanodiamond containing a spin

## Slide 79
- Berlin: atmospheric pressure, NV- florescence,
A Kuhlicke, AW Schell, J Zoll & O Benson, APL 105, 073101 (2014)
- Paris: atmospheric pressure, Optically-detected magnetic resonance,
T Delord, L Nicolas, L Schwab & G Hétet, NJP 19, 033031 (2017)
- University College London: Peter Barker‘s group
- Pittsburgh: 6.7 x 10-3 mbar, NV- florescence,
J-F Hsu, P Ji, CW Lewandowski & B D’Urso, Sci Rep 6, 30125 (2016)
- Rochester: 1064 nm, >5 mbar,
LP Neukirch, E von Haartman, JM Rosenholm & AN Vamivakas,
Nat Photon 9, 653 (2015)
- Purdue: 1550 nm, >10 mbar
TM Hoang, J Ahn, J Bang & T Li, Nat Comms 7, 12250 (2016)
  Levitating nanodiamonds in air
Ion traps
Magneto-gravitational trap
Optical traps

## Slide 80
  Levitating nanodiamonds in air
ATMA Rahman et al., Scientific Reports 6, 21633 (2016)
AC Frangeskou et al., arXiv:1608.04724 (2016)
20 mbar

## Slide 81
Nitrogen-vacancy centres: Applications
Violating Bell’s inequality
The first experiment in which the “detection” and “locality” loopholes have both been closed
B Henson et al, Nature 526, 682 (2015)
Proposal for entangling remote NV-
SD Barrett and P Kok, Physical Review A 71, 060310 (2005)

## Slide 82
Silicon-vacancy centres
Better optical properties, worse spin properties (spin T2* ~ 45 ns)
  70% of the florescence from the SiV- is in the zero phonon line (ZPL), compared with 4% for NV- at low temperature
Spin control with coherent population trapping:
B Pingault et al, Physical Review Letters 113, 263601 (2014)
LJ Rogers et al, Physical Review Letters 113, 263602 (2014)

## Slide 83
Experiments with spin qubits in diamond: overview
Diamond
  Nitrogen-vacancy (NV) centre
    1. Properties
    2. Applications
    a) magnetometry
    b) thermometry
    c) electrometry
    d) in a tractor beam
    e) violating Bell’s inequality
  Silicon-vacancy (SiV) centre

## Slide 84
Quantum technology with diamond & silicon
Solid state physics background (diamond and silicon)
Magnetic resonance background
Spin qubits in silicon
Spin qubits in diamond

## Slide 85
Quantum technology with diamond & silicon
Nitrogen
Vacancy