## Slide 1: Gavin W Morley Department of Physics University of Warwick
Diamond Science & Technology
Centre for Doctoral Training, MSc course
Module 8 – Photonics and Quantum Technologies
Module 2 – (PX907)
Lectures 13 and 14 – Diamond Sensors based on nitrogen vacancy centres

## Slide 2
Diamond properties

## Slide 3
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 4
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 5
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 6
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 7
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 8
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 9
Sensing
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 10
Classical Sensing
With classical sensors, the signal to noise improves as
(for random noise i.e. the signal is uncorrelated to the noise, and the noise is uncorrelated)
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 11: Sensitivity
The minimal change in the measured quantity that can be resolved above the noise
A quantity (e.g. a magnetic field in Tesla) is measured as B, and its uncertainty in a single measurement is δB. Averaging over N measurements gives the average:
,
and its uncertainty:

## Slide 12: Sensitivity (cont.)
(1) The signal to noise ratio,
(2) The number of measurements is the measurement rate (R ) times the total measurement time (T ): N = R T , so
.
We define the sensitivity in measuring B as:
,
which has units of [B ].Hz-½ so for a magnetic field sensor it’s T.Hz-½

## Slide 13
Quantum Sensing
UΦ
UΦ
Use superposition
Use entanglement
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 14
Quantum Sensing
classical sensors: SNR improves as
quantum sensors: SNR can improve as
But it requires entanglement, and imperfections lower the quantum advantage
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 15
Practical Quantum Sensing
Don’t use maximally entangled states because of decoherence
Quantum sensing is useful when averaging is limited e.g. by size, time, fragile samples
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 16
Practical Quantum Sensing
  Magnetometry
  Thermometry
  Accelerometers
  Gravimetry
  Microscopy
  Imaging
Notes: Signal, SNR, resolution (temporal and spatial)

## Slide 17
Quantum Sensors
Cold atom interferometers
  Gravity, magnetic field, time, rotation
Ion trap
  Magnetic field, time
Atomic vapour cell
  Magnetic field
Nitrogen vacancy centres in diamond
  Magnetic field, electric field, temperature
Optical spectroscopy of atoms
Optical spectroscopy of atoms
Optical spectroscopy of atoms
Optical spectroscopy of atoms

## Slide 18
Quantum Sensors
Cold atom interferometers
  Gravity, magnetic field, time, rotation
Ion trap
  Magnetic field, time
Atomic vapour cell
  Magnetic field
Nitrogen vacancy centres in diamond
  Magnetic field, electric field, temperature
Single atom or many?

## Slide 19
Quantum Sensors
for gravity
(also time, rotation and magnetic fields)
UK cost of digging up the roads : £5bn/yr

## Slide 20
AOSense (from Mark Kasevich lab, Stanford, California, 2010)
Muquans, Paris, 2016
Kai Bongs, Birmingham Hub, 2015
Quantum Sensors
for gravity
(also time, rotation and magnetic fields)

## Slide 21: Ion magnetometer
N-ion array chip fabricated by B. Lekitsch, Sussex

## Slide 22
Atomic vapour cells for sensing
magnetic fields
Twinleaf:
QuSpin:
Very good sensitivity in zero magnetic field (with magnetic shielding)

## Slide 23
    1. Properties
      Geometric structure
      Optical properties
      Spin properties
      Energy levels and transitions
    2. Magnetometry
Nitrogen-Vacancy Centres
Nitrogen-vacancy (NV-) centre

## Slide 24
Nitrogen-vacancy (NV-) centre
Geometric structure
Diamond, from John Singleton
Carbon atoms
Missing carbon
Nitrogen atom
NV- Review paper: MW Doherty, NB Manson, P Delaney, F Jelezko, J Wrachtrup, LCL Hollenberg, Phys Rep 528, 1 (2013)

## Slide 25
Optical properties of NV- centres
Photograph by Jon Newland (Warwick)

## Slide 26
Optical properties of NV- centres
Confocal microscope image
Photograph by Jon Newland (Warwick)

## Slide 27
Spin properties of NV- centres
Green excitation 
1. Spin polarization
2. Spin-dependent florescence
Review:
L Rondin et al., Magnetometry with nitrogen-vacancy defects in diamond, Rep Prog Phys 77, 056503 (2014)

## Slide 28
Nitrogen-vacancy (NV-) energy levels
3A2
3E
1A1
1E
±1
±1
±0
±0
Red names come from the C3v point group: see appendix of Doherty et al
Black numbers are spin state (in zero magnetic field)

## Slide 29
3A2
3E
1A1
1E
±1
±1
±0
±0
Green excitation
Nitrogen-vacancy (NV-) energy levels

## Slide 30
3A2
3E
1A1
1E
±1
±1
±0
±0
Red Emission
Decay time ~12ns
Nitrogen-vacancy (NV-) energy levels

## Slide 31
3A2
3E
1A1
1E
±1
±1
±0
±0
Microwave excitation (2.9 GHz)
Nitrogen-vacancy (NV-) energy levels

## Slide 32
3A2
3E
1A1
1E
±1
±1
±0
±0
Green excitation
Nitrogen-vacancy (NV-) energy levels

## Slide 33
3A2
3E
1A1
1E
±1
±1
±0
±0
No red florescence (only IR), decay time >300 ns
Nitrogen-vacancy (NV-) energy levels

## Slide 34
Green excitation 
1. Spin polarization
2. Spin-dependent florescence
Nitrogen-vacancy (NV-) energy levels

## Slide 35
Nitrogen-vacancy centres: Applications
DC Magnetometer
Energy of NV-
Magnetic field, B0
ms = +1
ms = -1
ms = 0
2.88 GHz
Review:
L Rondin et al., Magnetometry with nitrogen-vacancy defects in diamond, Rep Prog Phys 77, 056503 (2014)

## Slide 36
Nitrogen-vacancy centres: Applications
DC Magnetometer
Energy of NV-
Magnetic field, B0
ms = +1
ms = -1
ms = 0
D = 2.88 GHz
with

## Slide 37
Magnetic field, B0
ms = +1
ms = -1
ms = 0
15 pT.Hz-½ sensitivity at 80 - 2000 Hz from (13 x 200 x 2000) µm3 diamond: JF Barry et al., PNAS 2016
Nitrogen-vacancy centres: Applications
DC Magnetometer
Energy of NV-
Bulk, DC, lock-in

## Slide 38
Lock-in detection
Magnetic field, B
Magnetic field modulation
(~1 to 100 kHz)
Advantage: noise only at
modulation frequency
Signal
Lock-in signal
Bulk, DC, lock-in

## Slide 39
Nitrogen-vacancy centres: Applications
DC Magnetometer: lock-in detection
H Clevenson et al, Nat Phys 11, 393 (2015)
Bulk, DC, lock-in

## Slide 40
15 pT.Hz-½ sensitivity at 80 - 2000 Hz from (13 x 200 x 2000) µm3 diamond: JF Barry et al., PNAS 2016
Nitrogen-vacancy centres: Applications
DC Magnetometer
Bulk, DC, lock-in

## Slide 41
H Clevenson et al, Nat Phys 11, 393 (2015)
Barry et al
JF Barry et al., PNAS 2016
Nitrogen-vacancy centres: Applications
DC Magnetometer
Bulk, DC, lock-in

## Slide 42
Nitrogen-vacancy centres: Applications
Warwick: bulk magnetometry towards medical imaging
Bulk, DC, lock-in

## Slide 43
Single nitrogen-vacancy centres
Ramsey interferometry
Review:
L Rondin et al., Magnetometry with nitrogen-vacancy defects in diamond, Rep Prog Phys 77, 056503 (2014)
Bulk, DC, beyond lock-in

## Slide 44
Review:
L Rondin et al., Magnetometry with nitrogen-vacancy defects in diamond, Rep Prog Phys 77, 056503 (2014)
Single nitrogen-vacancy centres
AC magnetometry
AC, pulsed readout

## Slide 45
Spin echo
In rotating frame
Spin echo
AC, pulsed readout
Notes: Hahn echo

## Slide 46
Spin echo
In rotating frame
Spin echo
AC, pulsed readout
Notes: Hahn echo

## Slide 47
Single nitrogen-vacancy centres
Spin coherence times
 | Electron spin in 12C | Nuclear spin
Room temperature T2 | 1.8 ms | 1 s
cryogenic T2 | 0.6 s (with decoupling) | 10 s
1.8 ms: G Balasubramanian et al, Nature Materials 8, 383 (2009)
0.6 s: N Bar-Gill et al, Nat Commun 4, 1743 (2013)
1 s: PC Maurer et al, Science 336, 1283 (2012)
10 s: S Yang et al, Nature Photonics 10, 507 (2016)
AC, pulsed readout

## Slide 48
Nitrogen-vacancy centres: Applications
Bulk AC Magnetometer
- Spin echo on the NV- centre allows through chosen frequency of interest
- Ensemble of ~1011 NV-
1 pT/√Hz sensitivity at 10 kHz:
T Wolf et al, Phys. Rev. X 5, 041001 (2015)
Bulk AC, pulsed readout

## Slide 49
Nanoscale magnetometer for NMR
AC detection of single proton spin on surface of diamond in ambient conditions:
AO Sushkov et al, Phys Rev Lett 113, 197601 (2014)
also
6 nT Hz-½ DC (20 Hz) with wide dynamic range of 1.7 mT:
C Bonato et al, Nature Nanotechnology 11, 247 (2015)
AC detection at ~200 kHz:
T Staudacher et al, Science 339, 561 (2013)
Nitrogen-vacancy centres: Applications
Single NV, AC, pulsed readout

## Slide 50
Warwick: single spin magnetometry
Nitrogen-vacancy centres: Applications
Single NV, AC, pulsed readout

## Slide 51
Nanoscale magnetometer for scanning over a sample
Nitrogen-vacancy centres: Applications
P. Maletinsky et al., Nature Nano. 7, 320 (2012)
Single NV, AC, pulsed readout

## Slide 52
Nanoscale AC magnetometer for scanning over a sample
- Dynamic decoupling allows through chosen frequency of interest
Detect a single electron spin 50 nm away from NV- sensor:
MS Grinolds et al, Nat Phys 9, 215 (2013)
Nitrogen-vacancy centres: Applications
Single NV, AC, pulsed readout

## Slide 53
Wide-field magnetometry
Optical magnetic imaging of living cells, D Le Sage et al, Nature 496, 486 (2013)
Diamond is bio-compatible
Nitrogen-vacancy centres: Applications

## Slide 54
Nitrogen-vacancy centres: Summary
    1. Properties
      Geometric structure
      Optical properties
      Spin properties
      Energy levels and transitions
    2. Applications
      Magnetometry
        DC vs AC
        Bulk vs nanoscale
        Room temperature vs cryogenic
        Scanning vs widefield

## Slide 55
Nanoscale thermometry for inside living cells & computer chips
G Kucsko et al, Nature 500, 54 (2013)
P Neumann et al, Nano Lett 13, 2738 (2013)
DM Toyli et al, PNAS 110, 8417 (2013)
Nitrogen-vacancy centres: Applications
with
and βT = 74 kHz/K

## Slide 56
Electrometry: Stark shift
F Dolde et al, Nat Phys 7, 459 (2011)
Nitrogen-vacancy centres: Applications

## Slide 57
Violating Bell’s inequalities
The first experiment in which the “detection” and “locality” loopholes have both been closed
B Henson et al, Nature 526, 682 (2015)
Proposal for entangling remote NV-
SD Barrett and P Kok, Physical Review A 71, 060310 (2005)
Nitrogen-vacancy centres: Applications

## Slide 58
Conclusions: Quantum Sensors
Cold atom interferometers
  Gravity, magnetic field, time, rotation
Ion trap
  Magnetic field, time
Atomic vapour cell
  Magnetic field
Nitrogen vacancy centres in diamond
  Magnetic field, electric field, temperature
  Optical spectroscopy of atoms
  Single atom vs many